## Slide 1: Cladding Model Development For Time at Temperature
L. Capolungo, A. Rovinelli, M-J. Chen, N. Millitello, S. Blondel, B. Wirth

## Slide 2: T@T: Problem Statement
Question: What is the impact of a T@T event on the mechanical performance of Zircaloy cladding?
Challenge: Several microstructure evolution processes will be activated during T@T:
Dislocation line recovery
Irradiation loop recovery
Recrystallization
Precipitations, etc.
All of these processes depend on the microstructure of the material when T@T occurs.
How to quantify the relative and absolute roles of each of these processes on mechanical performance?
Zircaloy 4: Microstructure at 200C*
Zircaloy 4: Microstructure after temperature hold at 800C*
* Courtesy of B. Eftink

## Slide 3: T@T Strategy: Mechanistic Multiscale Models Can be Used to Predict and Rationalize T@T
LApx polycrystal simulation solver for the mechanical response of materials.
LApx captures:
Grain size effects,
Texture,
Dislocation (storage, recovery)
Precipitate (hardening)
Solutes (strengthening)
Irradiation hardening
LApx captures the tensile response of Zircaloy as a function temperature.
The creep response as a function of temperature and stress
Future extensions:
Recrystallization
Cluster dynamics coupling
experiment
[1,2]
~4
~1
~9

## Slide 4: T@T strategy: mechanistic multiscale models can be used to predict and rationalize T@T
LAROMance are microstructure sensitive surrogate models for the response of metals under arbitrary loading scenarios
A LAROMance Zircaloy model was developed and integrated in MOOSE/BISON
LAROMance Zircaloy is found to be able to blindly predict off normal loading scenarios (Rebeka tests)
Future extensions:
Generalize LAROMance to capture grain size, precipitate and irradiation effects
REBEKA tests: Validation of LApx approach
Courtesy of R. Sweet
Burst simulation using LAROMance
The idea: Both Microstructure informed polycrystal (LApx) and surrogate models (LAROMance) can be used to study and rank the likely impact of different microstructure features on the response post T@T

## Slide 5
Predicts the behavior of composite and engineering materials, including damage and ductile failure (for any constitutive model), under extreme environments
  Creep
  Fatigue
  Complex Loadings
  Chemo-mechanical solver
  Cyclic load
Zecevic, Lebensohn, Capolungo, MoM, 2022
Ageing
(thermal irradiation)
Dislocation glide
(Cross slip, DSA)
Vacancy diffusion mediated plasticity
Damage nucleation growth coalescence
LApx: A High Fidelity and Numerically Efficient Polycrystal Code
MATERIAL FINGERPRINT
DISLOCATION CONTENT
DISLOCATION ARRANGEMENT (CELLS VS CELL WALLS)
SOLUTE CONTENT
NON EQUILIBRIUM POINT DEFECTS (INTERSITIALS, VACANCIES, CLUSTERS)
EQUILIBRIUM PRECIPITATES
NON-EQUILIBRIUM PRECIPITATES
TEXTURE
Grain MORPHOLOGY AND SIZE

## Slide 6
What is the role of irradiation loop recovery (assume full recovery takes place)?
What is the role of static recovery of dislocations?
What is the role of recrystallization?
Prior to develop models for the dynamic evolution of the microstructure, let us use LApx to bound the problem.

## Slide 7
at
Time at Temperature Effects

## Slide 8: Time at Temperature Effects
2 slides
at
Property | Min | Max | Effect on yield | Temperature effect on content
 | 1e12 | 1e15 |  | 
 | 1 | 15 |  | 
 | 0.125 | 0.5 |  | 
 | 0 | 5e20 |  | 
Property | Min | Max | Effect on yield | Temperature effect on content
 | 1e12 | 1e15 |  | 
 | 1 | 15 |  | 
 | 0.125 | 0.5 |  | 
 | 0 | 5e20 |  | 
Inverse effect
Direct effect
Increase density/size
Decrease density/size
Can we identify which microstructure features provides the largest change?
Static recovery
Effect of high t@T

## Slide 9: Time at Temperature Effects
2 slides
at
Strain accumulates over
property | Min | Max | Effect on yield | Temperature effect on content
 | 1e12 | 1e15 |  | 
 | 1 | 15 |  | 
 | 0.125 | 0.5 |  | 
 | 0 | 20 |  | 
property | Min | Max | Effect on yield | Temperature effect on content
 | 1e12 | 1e15 |  | 
 | 1 | 15 |  | 
 | 0.125 | 0.5 |  | 
 | 0 | 20 |  | 
Inverse effect
Direct effect
Increase density/size
Decrease density/size
Can we identify which microstructure features provides the largest change?
Static recovery
Different mechanical behavior

## Slide 10: Static Recovery:
property | Begin | End
 | 1e15 | 1e12
 | 1 | 1
 | 0.5 | 0.5
 | 5e20 | 5e20
property | Begin | End
 | 1e15 | 1e12
 | 1 | 1
 | 0.5 | 0.5
 | 5e20 | 5e20
The scenario represents only dislocation recovery
The reference is the strongest microstructure:
fine grain
high dislocation density
high precipitate density
and high density of dislocation loops (20 dpa).

## Slide 11: Hall Petch (Grain Size) Effect
We assume the transient will only change grain size without affecting other properties
property | Begin | End
 | 1e15 | 1e15
 | 1 | 15
 | 0.5 | 0.5
 | 5e20 | 5e20
property | Begin | End
 | 1e15 | 1e15
 | 1 | 15
 | 0.5 | 0.5
 | 5e20 | 5e20

## Slide 12: Precipitate Dissolution
We assume precipitate will dissolve and any other feature to stay the same
property | Begin | End
 | 1e15 | 1e15
 | 1 | 1
 | 0.5 | 0.125
 | 5e20 | 5e20
property | Begin | End
 | 1e15 | 1e15
 | 1 | 1
 | 0.5 | 0.125
 | 5e20 | 5e20

## Slide 13: Loop Recovery Effect:
Dislocation loops will dissolve during the high temperature transient
property | Begin | End
 | 1e15 | 1e15
 | 1 | 1
 | 0.5 | 0.5
 | 5e20 | 0
property | Begin | End
 | 1e15 | 1e15
 | 1 | 1
 | 0.5 | 0.5
 | 5e20 | 0

## Slide 14: Compounded Effects
The reference stress is selected as the condition with the highest yield stress to start with.
property | Reference | Min | Max
 | 1e15 | 1e12 | 1e15
 | 1 | 1 | 15
 | 0.5 | 0.125 | 0.5
 | 5e20 | 0 | 5e20
property | Reference | Min | Max
 | 1e15 | 1e12 | 1e15
 | 1 | 1 | 15
 | 0.5 | 0.125 | 0.5
 | 5e20 | 0 | 5e20

## Slide 15: Comparison with Experimental Data
Hardness is directly proportional to yield
The range of variation in the yield strength is within the range of the variation observed in from LApx simulations
[1] Courtesy of Nathan Caps ORNL
[1]

## Slide 16: Comparison with Experimental Data
Hardness is directly proportional to yield
The range of variation in the yield strength is within the range of the variation observed in from LApx simulations
[1] Courtesy of Nathan Caps ORNL
[1]
Which features provides the greatest contribution to recovery?

## Slide 17: Contribution to Yield Reduction
1
2
3
4
Dislocation recovery provides the largest change in yield strength (~30%)
Precipitate dissolution ~10%
Hall-Petch (grain size) ~5%
During dynamic recrystallization dislocation recovers because of:
  Annealing
  GB migration
Recrystallization is a dynamic effect that need to be included to include the dynamic effect time at temperature

## Slide 18
Can irradiation induced loops evolve drastically during T@T?

## Slide 19: Xolotl α-Zr Overview
J. F. March-Rico, “Scale Bridging Computational Modeling of Irradiation Effects in Alpha-Zirconium and its Alloys,” University of Tennessee, 2022
Cluster dynamics model that describes microstructural change of α-Zr through rate theory approach
  Key model parameters informed through DFT, MS, and MD simulations rather than simplifying assumptions
    Defect cluster production directly in energetic cascades
    dislocation loop binding energies
    defect capture radii
    mobile defect diffusivity and anisotropy
Simultaneous nucleation and growth of vacancy and interstitial a-type dislocation loops achieved through bias for self capture
Vacancy c-loops introduced through evolution of pyramidal defects introduced directly in energetic cascades
  Strongly correlated with rapid ‘breakaway’ growth mechanism

## Slide 20
5 dpa
final vac a-loop
defect density: 1.664e+21 m-3
atom density: 7.338e+24 m-3
avg diameter: 20.545 nm
5 dpa
post ramp
final vac a-loop
defect density: 5.691e+21 m-3
atom density: 5.671e+25 m-3
avg diameter: 32.52 nm
Microstructure Changes During T@T: Irradiation Loops

## Slide 21
5 dpa
final vac a-loop
defect density: 1.664e+21 m-3
atom density: 7.338e+24 m-3
avg diameter: 20.545 nm
5 dpa
post ramp
final vac a-loop
defect density: 5.691e+21 m-3
atom density: 5.671e+25 m-3
avg diameter: 32.52 nm
Microstructure Changes During T@T: Irradiation Loops

## Slide 22
final basal
defect density: 1.873e+17 m-3
atom density: 1.541e+21 m-3
avg diameter: 11.849 nm
5 dpa
20 K/s ramp
to 1100K
w/ irrad.
final vac a-loop
defect density: 1.664e+21 m-3
atom density: 7.338e+24 m-3
avg diameter: 20.545 nm
final basal
defect density: 2.01e+16 m-3
atom density: 1.33e+21 m-3
avg diameter: 87.241 nm
final int a-loop
defect density: 2.09e+21 m-3
atom density: 7.025e+24 m-3
avg diameter: 17.3 nm
5 dpa
post ramp
final vac a-loop
defect density: 5.691e+21 m-3
atom density: 5.671e+25 m-3
avg diameter: 32.52 nm
final int a-loop
defect density: 7.810e+21 m-3
atom density: 5.626e+25 m-3
avg diameter: 17.844 nm
Microstructure Changes During T@T: Irradiation Loops

## Slide 23
Summary of work done:
Bounded the likely effects of microstructure change on T@T
Recrystallization likely plays a dominant role on the T@T due to annealing
Irradiation loop recovery and precipitation are important but secondary
No further strain accumulation
Transients begins
Beginning of hold
End of hold
Next steps:
Develop a recrystallization model
Improve the Cluster dynamics code to quantify loop recovery post T@T
Conclusions

## Slide 24
laurent@lanl.gov