## Slide 1: Incorporating irradiation effects in predictive models of Grade 91 alloy
V. Vivekanandan, J. Joy, A. Talapatra, L. Capolungo

## Slide 2: NEAMS developed ready to use capabilities to predict the post-irradiation and in situ response of Ferritic Martensitic steel
Effect of microstructure on mechanical performance?
Response of material under irradiation?
Takeway message:
We can predict the performance envelope of Grade 91 during tensile and creep loads.
How we can relate the mechanical performance of RAFMs to their microstructure (including the loss of high temperature strength).
Predict the post irradiation response of Ferritic/Martensitic steels.
Predict the in-pile response of Ferritic Martensitic steels.
Time to critical strain

## Slide 3: Objective: develop models to (i) extrapolate the mechanical response and failure of materials under extreme environments, (ii) quantify how micvrostructure affect behavior.
Example of a ferritic-martensitic microstructure
*F. ABE, Advanced Steels, Chapter 11, 2011
Composition:
9Cr, 1Mo, VNb
FM steel are strengthened by lat boundaries, solutes and precipitates. Hoe can we quantify the efficacy of each strengthener ads a function of temperature and irradiation damage?
*Similar approaches are pursued to study HT9, 316H, additively manufactured steels, superaloys, Zircaloys.

## Slide 4: Idea: Use a multiscale modeling approach to capture how each deformation mechanism is affected by microstructure and constraints
Applicability of the models
  Creep
  Fatigue
  Complex Loadings
  Chemo-mechanical solver
  Cyclic load
Zecevic, Lebensohn, Capolungo, MoM, 2022
Ageing
(thermal irradiation)
Dislocation glide
(Cross slip, DSA)
Vacancy diffusion mediated plasticity
Damage nucleation growth coalescence
*Caveat: in all future slides, the lath size, precipitate content and irradiation induced defects content are not evolving dynamically

## Slide 5: A universal model for the effects of temperature on the tensile and creep response of Gr91
LApx captures anomalous temperature effects on yield and ultimate strength of Gr91 and the creep response simultaneously over a wide range of stresses and temperatures
glide
climb
diffusion

## Slide 6: How microstructure affects mechanical performance of Gr91 under thermal conditions: assessment of performance variability
Quantification of the effect of microstructure on Variability in performance of Gr91.
After climb
A new postulate: Coupling between dislocation climb and can lead to loss of creep strength in alloys strengthened by small precipitate
Our model can blindly predict the variability in creep response (minimum creep rate) induced by variability in initial microstructure.
The effect of microstructure (i.e. lath size, precipitate content, dislocation density) on performance variability depend on stress and temperature.
We reveal that the loss of strength at high temperatures is due to a mechanisms of bypass of precipitates by dislocations

## Slide 7
dpa | Black dot density(), size (m) | Loop density(), size (m)
0.06 | 2e22, 2e-9 | 2e21,15e-9
1.5 | 2e22, 2e-9 | 2e21, 9e-9
10 | 1.9e22,2e-9 | 2e20,7e-9
dpa |  | 
0.06 | 2e22, 2e-9 | 2e21,15e-9
1.5 | 2e22, 2e-9 | 2e21, 9e-9
10 | 1.9e22,2e-9 | 2e20,7e-9
LApx can predict the post irradiation response of T91 as a function of dose
*Ongoing work aims at dynamically predicting the evolution of microstructure induced by damage. The microstructure is taken as an input for now

## Slide 8
In pile
Out of pile
LApx can predict the post irradiation response of T91 as a function of dose

## Slide 9: We identified the mechanism leading to creep acceleration under irradiation
After climb

## Slide 10: NEAMS developed ready to use capabilities to predict the post-irradiation and in situ response of Ferritic Martensitic steel
Takeway message:
We can predict the performance envelope of Grade 91 during tensile and creep loads.
How we can relate the mechanical performance of RAFMs to their microstructure (including the loss of high temperature strength).
Predict the post irradiation response of Ferritic/Martensitic steels.
Predict the in-pile response of Ferritic Martensitic steels.

## Slide 11
laurent@lanl.gov