## Slide 1: Structural Materials and Chemistry Technical Area Overview: Light Water Reactors
Benjamin Spencer1 and Ted Besmann2
1Idaho National Laboratory
2University of South Carolina
Contact: Benjamin.Spencer@inl.gov

## Slide 2: Technical Area Overview
Nuclear reactors contain numerous structural components, the integrity of which is essential for their safe and reliable operation
The Structural Materials & Chemistry Technical Area is developing computational tools for two main applications:
  Ensuring the integrity of structural components in current and advanced reactors
  Chemistry modeling in molten-salts, including speciation, depletion, corrosion, and plating.
The tools being developed are designed to integrate with the other tools being developed by the NEAMS program for seamless multiphysics coupling

## Slide 3: Research Topics and Codes
Structural Material Performance
Molten-Salt Chemistry
High-Temperature Alloy Creep1
LAROMANCE/LApx NEML2 Grizzly/BlackBear
Reinforced Concrete Degradation Grizzly/BlackBear
Graphite Components2 Grizzly
Fast-Reactor Core Duct Deformation
MOOSE
Databases MSTDB-TP
MSTDB-TC3
Gibbs Energy Minimizer Thermochimica/
MOOSE
Transport Codes Mole
Pronghorn MOSCATO
Ab-initio Salt Property Prediction
AIMD, MD, MD with ML potentials
LWR Reactor Pressure Vessel Integrity Grizzly
3Developed by MSR program
Metal Hydride Moderators SWIFT
1Coordination with AMMT program
2Data from ART program

## Slide 4: Research Topics and Codes (Presentation Topics Indicated)
Structural Material Performance
Molten-Salt Chemistry
High-Temperature Alloy Creep1
LAROMANCE/LApx NEML2 Grizzly/BlackBear
Reinforced Concrete Degradation Grizzly/BlackBear
Graphite Components2 Grizzly
Fast-Reactor Core Duct Deformation
MOOSE
Databases MSTDB-TP
MSTDB-TC3
Gibbs Energy Minimizer Thermochimica/
MOOSE
Transport Codes Mole
Pronghorn MOSCATO
Ab-initio Salt Property Prediction
AIMD, MD, MD with ML potentials
LWR Reactor Pressure Vessel Integrity Grizzly
3Developed by MSR program
Metal Hydride Moderators SWIFT
1Coordination with AMMT program
2Data from ART program

## Slide 5: Reinforced Concrete Degradation
Reinforced concrete (RC) structures play a key role in LWR safety and are a major capital investment
Important mechanisms in nuclear structures:
  Creep
  Alkali-silica reaction (ASR)
  Radiation-induced volumetric expansion (RIVE)
NEAMS Modeling tools:
  BlackBear (open source): foundational capabilities
  Grizzly: Everything in BlackBear, plus RIVE
Fracture in concrete containment vessel cut for repair (Image from Progress Energy, NRC ML09320292)
Cracking due to ASR in a concrete containment vessel (Image from NRC, ML12199A300)

## Slide 6: Processes Affecting Alkali-Silica Reaction
ASR modeling starts with the underlying processes:
  Temperature
  Moisture
  Mechanical Deformation
Coupled-physics models for evolution and interaction of these processes
Model predicts deformation and degradation due to ASR
  Initial state for capacity assessment
Moisture
Temperature
Mechanical Deformation
ASR & Associated Expansion/Damage

## Slide 7: Simulated ASR Effect on LWR RC Containment Vessel
Recent DOE Nuclear Safety R&D project used NEAMS tools to assess effects of ASR on seismic capacity
Unified modeling approach
  Model of prototypical LWR RC containment vessel with individual rebars represented
  Coupled-physics model for long-term progression of ASR and resulting damage
  Seismic response modeled following ASR
  Probabilistic analyses on hundreds of samples for seismic fragilities

## Slide 8: ASR Effect on Seismic Capacity
Long-term alkali-silica-reaction (ASR) damage to containment vessel
Damage after seismic loading (left) with ASR and
(right) without ASR
ASR effect on seismic fragility under multiple limit states
ASR Effect
A. Dahal, B. W. Spencer, S. L. Dhulipala, A. Jain, and L. F. Ibarra. Coupled alkali-silica-reaction/seismic simulation of nuclear containment vessels. International Journal of Mechanical Sciences, 110185, Apr. 2025.

## Slide 9: LWR Reactor Pressure Vessel Integrity
Reactor pressure vessels (RPVs) can contain large numbers of manufacturing flaws
  Most of the flaws are inconsequential
  Flaws can serve as fracture initiation sites
Rapid-cooling transients can challenge RPV integrity
  Elevated tensile stress
  Decreased toughness
Exposure to neutron irradiation embrittles the RPV steel
  Increased susceptibility to fracture over time
  RPVs are considered life-limiting reactor components
Grizzly capabilities for RPV fracture
  3D probabilistic assessment of sampled populations of flaws

## Slide 10: Assessing Spatially Nonuniform Cooling Using Coupled Fluid Dynamics and Fracture Mechanics
Cooling during transients can be highly spatially nonuniform
Most RPV probabilistic fracture mechanics models assume spatially uniform cooling
NEAMS effort coupled codes to simulate nonuniform cooling:
  NekRS: Computational fluid dynamics model of coolant within RPV
  Cardinal: Thermal coupling between coolant and RPV wall
  Grizzly: Probabilistic fracture of RPV
Computational fluid dynamics simulation of RPV wall temperatures during medium break loss of cooling accident (MBLOCA)

## Slide 11: Grizzly Probabilistic Fracture Model Shows Significant Effects from Nonuniform Cooling
Three scenarios considered:
  Average coolant temperature uniformly applied (non-conservative, current practice)
  Spatially varying temperature (most accurate)
  Minimum coolant temperature uniformly applied (highly conservative)
Time history of maximum conditional probability of fracture initiation (CPI)
Flaws with nonzero CPI from 100,000 realizations shown on 90o RPV rollout. Critical flaws in regions with rapid cooling.

## Slide 12: Ongoing & Potential Future Efforts for RPV & Concrete
Both RPV and concrete simulation tools now have most major features
Concrete capability gap: models for rebar/concrete bond
  Current FY25 effort is adding bond-slip capability
Other potential areas for future research & development, depending on interest:
  Concrete:
    More sophisticated damage models (being developed for graphite modeling efforts)
    Other degradation mechanisms (e.g., chemical attack)
    Validation against experiments with combined ASR and mechanical loading
  RPV:
    Assessing relative importance of the various factors influencing fracture initiation in 3D plume model
    Models for predicting probability of full through-wall cracking, rather than initiation

## Slide 13: LWR-Relevant Fracture Modeling
Environmentally assisted fracture is important for LWR structural integrity
  Fractures in welds around penetrations in RPV head
  Stress-corrosion cracking in core internal components
Identified need for more robust tools for 3D fracture propagation into complex components
Ongoing development to address needs:
  Modeling methodology for residual stress development during welding processes
  Improve extended finite element method (XFEM) for both 2D and 3D mesh-independent fracture propagation into regions with residual stresses
Prior 2D and 3D applications of XFEM in MOOSE